First-Principles Electronic Transport Properties

of Ge/amorphous Al2O3/Au Structure

# Eunjung Ko1, Jaehong Park1,2, and Jung-Hae Choi1,*

1Center for Electronic Materials, Korea Institute of Science and Technology, Seoul 02792, Korea

2Department of Materials Science and Engineering, Seoul National University, Seoul 08826, Korea

# * E-mail: choijh@kist.re.kr

The Ge-based metal-oxide-semiconductor devices have Ge/high-k dielectric oxide/metal gate structures. Although many experimental studies on the gate leakage current of these structures have been performed in terms of the scaling down issues, first-principles theoretical works on the tunneling current density and, even, electronic structures have been rarely reported. Therefore, we investigate the first-principles electronic structures and the tunneling effect through the potential barrier of high-k oxide. The Ge/a-Al2O3/Au structure was chosen as a model system and three different nanometer scale thicknesses of a-Al2O3 are considered. The electronic transport properties of the Ge/a-Al2O3/Au structure are compared with those of the Ge/a-Al2O3/Ge structure. The tunneling effect under a positive and negative bias in Ge/a-Al2O3/Au structures is also presented thus the current vs. bias voltage characteristic curve is shown.