Antiferromagnetic Ordering in 2-Dimensional van der Waals Materials

Hyeonsik Cheonga

a Department of Physics, Sogang University

Magnetism in low dimensional systems is attracting much interest not only for the fundamental scientific interest but also as a promising candidate for numerous applications. Intense interest in 2 dimensional magentism has been stimulated by the discovery of ferromagnetism in atomically thin materials [1,2], but antiferromagnetic ordering is much more difficult to study because the lack of net magnetism hinders easy detection of such phenomena. Neutron scattering, which is a powerful tool to detect antiferromagnetic order in bulk materials, cannot be used for atomically thin samples due to the small sample volume. Raman spectroscopy has proven to be a powerful tool to detect antiferromagnetic ordering by monitoring the zone-folding due to the antiferromagnetic order [3,4] or the signal from two magnon scattering. In this talk, I will review recent achievements in the study of antiferromagnetism in 2 dimensions using Raman spectroscopy. FePS3 exhibits an Ising-type antiferromagnetic ordering down to the monolayer limit, in good agreement with the Onsager solution for 2-dimensional order-disorder transition. The transition temperature remains almost independent of the thickness from bulk to the monolayer limit, indicating that the weak interlayer interaction has little effect on the antiferromagnetic ordering. [4] On the other hand, NiPS3, which shows an XXZ-type antiferromagnetic ordering in bulk, exhibits antiferromagnetic ordering down to 2 layers, but the magnetic ordering is suppressed in the monolayer limit. [5]

# References

[1] C. Gong, et al., Nature 546, 265 (2017).

[2] B. Huang, et al., Nature 546, 270 (2017).

[3] X. Wang, et al., 2D Materials 3, 031009 (2016).

[4] J.-U. Lee, H. Cheong, et al., Nano Letters 16, 7433 (2016).

[5] K. Kim, H. Cheong, et al., in revision.